## Slide 1: NTM: ELECTRO DISCHARGE MACHINING ME 270
Dr. G. TAKYI

## Slide 2: INSTRUCTIONAL OBJECTIVE
Identify electro-discharge machining (EDM) as a particular type of non-tradition processes
Describe the basic working principle of EDM process
Draw schematically the basics of EDM
Describe spark initiation in EDM
Describe material removal mechanism in EDM
Draw the basic electrical waveform used in EDM
Identify the process parameters in EDM
Describe the characteristics of EDM
Identify the purpose dielectric fluid in EDM
List two common dielectric fluid

## Slide 3: INSTRUCTIONAL OBJECTIVES
Analyze the required properties of EDM tool
List four common tool material for EDM
Develop models for MRR in EDM
Identify machining characteristics in EDM
Analyze effect of process variable son roughness
Analyze taper cut and over cut in EDM
Identify different modules of EDM systems
Draw schematic representation of different electrical generators used in EDM
Analyze working principle of RC type EDM generator

## Slide 4: Classification of NTM Processes
Mechanical Processes
  abrasive Jet Mechanism (AJM)
  Ultrasonic Machining (USM)
  Water Jet Machining (WJM)
Electrochemical Processes
  Electrochemical Machining (ECM)
  Electro Chemical Grinding (ECG)
  Electro Jet Driling (EJD)

## Slide 6: Mechanism of Material Removal
Potential differences
Generally tool negative and work positive
Electric field is established
Tool and work piece-conductor of electricity

## Slide 7
Mechanism of Material Removal (CONT’D)
This free electrons are available
If the work function is low, electrons get emitted from tool
Cold emission of electrons and acceleration of same
Collision of electron with dielectric molecules
Secondary and tertiary collision – plasma channel
Avalanche motion of electrons – spark
Impingement of work piece by high energy electron
High temperature on work piece
Shock wave – material removal

## Slide 9: Step waveform not continuous to get a spark not arc

## Slide 10: Parameters, ton, toff, Voc, Vw

## Slide 12: Process Parameters in EDM
The open circuit voltage – Vt
The working voltage – Vh
The maximum current – Io
The pulse on time – ton
The pulse off time – toff
The gap between the work piece and the tool – spark gap - ȸ
The polarity – straight polarity – tool (-ve)
The dielectric medium
External flushing through the spark gap.

## Slide 14: Characteristics of EDM
The process can be used to machine any work material if it is electrically conductive
Material removal depends on mainly thermal properties of the work material rather than its strength, hardness etc

## Slide 15
Characteristics of EDM
In EDM there is a physical tool and geometry of the tool is the positive impression of the hole or geometric features to be machined
The tool has to be electrically conductive as well. The tool wear once again depends on the thermal properties of the tool material

## Slide 16
Characteristics of EDM
Through the local temperature rise is rather high, still due to very small pulse on time, there is not enough time for the heat to diffuse and thus almost no increase in bulk temperature takes place. Thus the heat affected zone is limited to 2-4 pm of the spark crater
However rapid heating and cooling and local high temperature leads to surface hardening which may be desirable in some applications

## Slide 18: TAPER CUT AND OVER CUT
Though there is a possibility

## Slide 26: PRODUCT QUALITY ISSUES IN EDM
Surface finish
Over Cut
Taper Cut

## Slide 29: EDM EQUIPMENT
Dielectric reservoir, pump and circulation system
Power generator and control unit
Working tank with work holding device
X-Y tube accommodating the working table
Tool holder
Servo system to feed the tool

## Slide 30: TYPES OF EDM GENERATORS
Resistance – Capacitance type (RC)
Rotary generator
Rotary impulse type generator
Electronic pulse generator
Hybrid EDM generator

## Slide 39: SUMMARY
Basic mechanism of material removal in EDM
Process parameters of EDM and defects on MRR
Different Quality Parameters and their control
Mathematical model relating MRR and surface roughness with EDM parameters
Major components of EDM equipment
Analysis of RC type generator

## Slide 40: QUIZ
Which of the following material cannot be maintained by EDM
  Steel
  WC
  Titanium
  Glass
Which of the following is used as dielectric medium in EDM
  Tap water
  Kerosene
  NaCl solution
  KOH Solution

## Slide 41: QUIZ
3. EDM tool should not have
  High machinability
  Low thermal conductivity
  High melting point
  High specific heat
4. EDM tool material should be
  Electrical insulator
  Electrically conductive
  Very hard
  thermal insulators

## Slide 42: SOLVED PROBLEM
In a RC type generator, the maximum charging voltage is 80 V and the charging capacitor is 100 μF. Determine spark energy.
Solution
=X 100 X X = 0.32 J